New York State Department of Health

Bureau of Community Environmental Health and Food Protection

Acceptable Encapsulant Products

# February, 2008

| Product Name | Manufacturer | Not Recommended | Dry Film Thickness | Respiratory Protection Required | Occupancy During an Application | States Approved In |
| --- | --- | --- | --- | --- | --- | --- |
| Back to Nature "Protect-A-Coat" | Dynacraft Industries Inc. Or Back to Nature Products Company 28 Harrison Avenue Englishtown, NJ 07726 (800) 922-0621 www.backtonatureprod.com | Walls or ceilings with chalking or calcimine paint Door jambs Window headers and stops Working radiators Friction surfaces Exterior surfaces | 7 mils minimum | For spray application, use molded polymesh shell dust and mist respirator - MSHA, NIOSH Approval No. TC-23C-287 or equivalent | Occupants must be out during the day for spray application only. Occupants may be in residence but not in room or work area undergoing encapsulation if brush or roller is used. Use adequate ventilation during the first 24 hours after application | CO, OH, MA, MI |
| Barrier Coat II | W.R. Grace & Co. 62 Whittemore Avenue Cambridge, MA 02140 (908) 531-3666 (800) 334-8796 www.na.graceconstruction.com | Walls with chalking or calcimine Door jambs Window headers and stops Ceilings with calcimine Working radiators Friction surfaces | 7 mils minimum (interior) 14 mils (exterior) | For spray application, use molded polymesh shell dust and mist respirator - MSHA, NIOSH Approval No. TC-21C-287 or equivalent | Occupants must be out during the day for spray application. Occupants may be in residence but not in room or work area undergoing encapsulation if brush or roller is used. Use adequate ventilation during the first 24 hours after application | CO, OH, MI |
| Insl-Cap Lead Encapsulating Compound | Insl-X Products Corp. 50 Holt Drive Stony Point, New York 10980 (845) 786-5000 www.insl-x.com | Walls or ceilings with chalking or calcimine paint Door jambs Window headers and stops Working radiators Friction surfaces Exterior surfaces | 7 mils minimum | For spray application, use molded polymesh shell dust and mist respirator - MSHA, NIOSH Approval No. TC-23C-287 or equivalent | Occupants must be out during the day for spray application only. Occupants may be in residence but not in room or work area undergoing encapsulation if brush or roller is used. Use adequate ventilation during the first 24 hours after application. | CO, OH, MA, MI |
| L-B-C Lead Barrier Compound (Type 1-Interior) | Fiberlock Technologies, inc 150 Dascomb Road Andover, Mass 01810 (800)342-3755 (978)623-9987 www.fiberlock.com | Walls with chalking or calcimine that have not been prepared with a surface conditioning product Door jambs Window headers/stops Ceilings with calcimine Working radiators where Surface temperatures Intermittently exceed 240 degrees F. Friction surfaces | 7 mils minimum | For spray application Use molded polymesh Shell dust and mist Respirator - MSHA, NOISH Approval No. TC-21C-287 or equivalent | Occupants must be out during the day for spray application only. Occupants may be in residence but not in room or work area undergoing encapsulation if brush or roller is used. Use adequate ventilation during the first 24 hours after application. | CO CT OH, MA |
| L-B-C Lead Barrier Compound (Type II - Exterior) | Fiberlock Technologies, Inc 150 Dascomb Road Andover, MA 01810 (800)342-3755 (978)623-9987 www.fiberlock.com | Walls with chalking or calcimine that have not been prepared with a surface conditioning product Door jambs Window headers/stops Ceilings w/calcimine Working radiators where surface temperatures intermittently exceed 240 degrees F. Friction surfaces | 7 mils minimum | For spray application, use molded polymesh shell dust and mist respirator - MSHA, NIOSH Approval No. TC-21C-287 or equivalent | Occupants must be out during the day for spray applications only. Occupants may be in residence but not in room or work area undergoing encapsulation if brush or roller is used. Use adequate ventilation during the first 24 hrs. after appl. | CO, CT |
| L-B-C Lead Barrier Compound Type III (Interior & Exterior) Or Childguard (Interior & Exterior) | Fiberlock Technologies, Inc 150 Dascomb Road Andover, MA 01810 (800)342-3755 (978)623-9987 www.fiberlock.com | Walls or ceilings with chalking or calcimine paint Door jambs Window headers and stops Working radiators Friction surfaces | 7 mils minimum | For spray application, use molded polymesh shell dust and mist respirator-MSHA, NIOSH Approval No. TC-23C-287 or equivalent | Occupants must be out during the day for spray application only. Occupants may be in residence but not in room or work area undergoing encapsulation if brush or roller is used. Use adequate ventilation during the first 24 hours after application. | CO, CT, OH, MI CT, OH, MA, MI |
| Lead-Master | Fiberlock Technologies, Inc 150 Dascomb Road Andover, MA 01810 (800)342-3755 (978)623-9987 www.fiberlock.com | Walls with chalking or calcimine that have not been properly prepared with a surface conditioning product Door jambs Window headers and stops Ceiling with calcimine Working radiators where the surface temperatures intermittently exceed 240 degrees F. Friction surfaces | 15 mils minimum | For spray application Use molded polymesh Shell dust and mist Respirator—MSHA, NOISH Approval No. TC-21C-287 or equivalent | Occupants must be out during the day for spray application only. Occupants may be in residence but not in room or work area undergoing encapsulation if brush or roller is used. Use adequate ventilation during the first 24 hours after application. | CO, CT, MA, MI |
| Lead Block | Coronado Paint Company, A division of Insul-X Products Corp. 2250 Arthur Avenue Elk Grove Village, IL 6007 (708) 439-4200 (800) 323-0633 www.coronadopaint.com | Walls with chalking or calcimine Door jambs Window headers, stops, and sills Ceilings with calcimine Working radiators if not top coated with alkyd or latex enamel Handrails and railing caps Cabinets and drawers Friction surfaces or removable closures | 14 to 16 mils | For spray application, use molded polymesh shell dust and mist respirator - MSHA, NIOSH Approval No. TC-23C-287 or equivalent | Occupants must be out during the day for spray application. Occupants may be in residence but not in room or work area undergoing encapsulation if brush or roller is used. Use adequate ventilation during the first 24 hours after application | CO, CT, OH, MI |
| LeadLock GE-40 | GLOBAL Encasement, Inc. PO Box 7724 North Bergen, NJ 07087 (201) 902-9770 (800) 266-3982 www.encasement.com | Walls with chalking or calcimine Door jambs Window headers, stops and sills Ceilings with calcimine Working radiators if not top coated with alkyd or latex enamel Handrails and railing caps Cabinets and drawers Friction surfaces or removable closures | 9 mils minimum for interior 18 mils minimum for exterior | For spray application Use molded polymesh Shell dust and mist Respirator—MSHA, NOISH Approval No. TC-21C-287 or equivalent | Occupants must be out during the day for spray application. Occupants may be in residence but not in room or work area undergoing encapsulation if Use adequate ventilation during the first 24 hours after application | CO, CT, OH, MI |
| Lead Stop | Dumond Chemicals 1501 Broadway, 26th Floor New York, New York 10036 (212) 869-6350 Fax (212) 764-5762 www.dumondchemicals.com or www.peelaway.com | High or constant friction areas such as window sash liners or door frames Walls with chalking or calcimine Door jambs Window headers and stops Ceilings with calcimine Working Radiators Frictions surfaces such as cabinets and drawers | 6 mils | Abide by OSHA regulations when using this product | Occupants must be out during the day for spray application. Occupants may be in residence but not in room or work area undergoing encapsulation if brush or roller is used. Use adequate ventilation during the first 24 hours after application | CO, OH, MA, MI |

P:Sections\Residentual\LEAD\ENCAPSUL\ENCAPCH42108